SECTION 09 84 13

FIXED SOUND-ABSORPTIVE PANELS

- – GENERAL

Specifier Note: Retain or delete paragraphs in Summary per project requirements.

  - SUMMARY

    - Section Includes:

      - Custom fabricated sound-absorptive wall panels.

      - Mounting accessories.

    - Related Sections:

      - Section 09 20 00 – Plaster and Gypsum Board

      - Section 09 70 00 – Wall Finishes

  - REFERENCES

    - ASTM C423 – Standard Test Method for Sound Absorption and Sound Absorption Coefficients by the Reverberation Room Method.

    - ASTM E84 – Standard Test Method for Surface Burning Characteristics of Building Materials

  - DEFINITONS

    - Noise Reduction Coefficient (NRC): Single number quantifier used to rate materials for their effectiveness in absorbing sound per ASTM C423.

  - SUBMITTALS

    - General: Provide listed submittals in accordance with Conditions of the Contract and Division 1 (Section 01 33 00) Submittal Procedures.

    - Product Data: Submit applicable reference standards, current performance data, application recommendations and product limitations.

    - Samples: Submit for approval two samples of the sound-absorptive panel not less than 12 inches by 12 inches.

    - Contract Closeout Submittals: (Refer to Section 01 78 00)

      - Operation (Section 01 78 23.13) and Maintenance Data (Section 01 78 23.16).

      - Warranty (Section 01 78 36) that all products shall perform in accordance with Contract Documents for a period of one (1) year from shipment and that any deficiencies shall be correctly promptly after receipt of written notice from Owner.

Specifier Note: Article below should include prerequisites, standards, limitations and criteria that establish an overall level of quality for products and workmanship for this section. Coordinate article below with Division 1 (Section 01 43 00) Quality Assurance.

  - QUALITY ASSURANCE

    - Installer's Qualifications: Installers shall have demonstrated experience in assembly and installation of products similar to those specified in this section.

    - Manufacturer's Qualifications: Manufacturer shall have demonstrated experience in fabrication of products similar to those specified in this section for a minimum of 5 years.

    - Fire Test Response Characteristics per ASTM-E84 Class A.

  - DELIVERY, STORAGE & HANDLING

    - General: Comply with Division 1 (Section 01 60 00) Product Requirements.

    - Delivery: Deliver materials in manufacturer’s original, unopened, undamaged containers with identification labels intact.

    - Storage and Protection: Store materials near installation point at temperature and humidity conditions recommended by the manufacturer.  Retain protective packaging.

  - FIELD CONDITIONS

    - Environmental Requirements: Do not install modules until all wet work is complete, the building is enclosed and temperature and humidity are similar to building conditions during occupancy.

- - PRODUCTS

  - MANUFACTURERS

    - Basis of Design: AAPG InkSonics AP1

      - AAPG, 248 James Street, Venice, FL 34285; Telephone: (844) 307-9571; E-mail: pwest@aapgco.com. Web site: www.millworkusa.com

    - Substitutions: No Substitutions permitted

  - Performance Requirements

    - Minimum Sound Absorption Coefficients for Type A Mounting: NRC 0.75

    - Panel shall be of a 1” thick with sufficient rigidity to provide a panel flatness which shall not exceed a deflection of L/240 inches as measured diagonally across the panel.

Specifier Note: Select applicable panel model and base material.  Delete any options which are not relevant.

  - MATERIALS

    - Panel Construction:

      - AP1: 1” thick. Hemp Core. Wrapped edges.

      - AP2: 1-1/4” thick. Hemp Core. Wrapped edges.

      - AP3: ¾” Thick. Hemp Core. Wrapped edges.

Specifier Note: Select applicable panel model, thickness and color range.  Delete any options which are not relevant.

  - FABRICATION

    - Hemp Cores shall be framed to provide frontal and rear air chamber

    - Panels edges shall be wrapped and rear sealed.

    - Color/Image: Per manufacturers standard range

  - ACCESSORIES

    - All trim and closure trim shall be aluminum concealed fastening.

- - EXECUTION

  - EXAMINATION

    - Verify that substrate conditions, which have been installed under other sections, are acceptable for product installation in accordance with manufacturer's instructions for installation.

    - Do not install panels until unsatisfactory conditions are corrected.

  - INSTALLATION

    - Comply with manufacturer's product data, installation instructions and product carton instructions for installation.

    - Install panels on room surfaces as indicated on the drawings.

  - CLEANING

    - Clean all surfaces according to manufacturer's recommendations.  Replace damaged components as directed by the Architect.

    - Remove all packaging and construction debris.

END OF SECTION